Wooden surface restoration guide

Surface maintanence

Surfaces treated with wood oils depending on environment conditions may need retreating as often as once a year.

Step-by-step guide

1. Brush off dirt, dust and lose material from the surface. Use a spatula for hard particles or resin.
2. Clean and wash mouldy spots with mould removal according to instructions. Wash vertical surfaces systematically from the bottom upwards to avoid runs. Let the surface dry.
3. Mask with film and masking tape the surfaces not treated, e.g., steel structure.
4. Carefully stir the paint. Cover the surface by using a painting brush. To avoid overlapping, apply the oil in continuous strokes to cover the whole surface evenly. Wipe off the excess oil from non-absorbing surfaces.
5. Clean the brush with white spirit or appropriate cleaner. Dispose soaked material with care, it can be self-inflammable.

To be considered

* The final surface colour depends on the species, hardness and original colour of the wood, and the number of times it has been treated.
* Mould Removal lightens wood surfaces considerably.
* Test a small area of similar wood before application.
* Surfaces treated with oil will finally cure and harden after a week in normal conditions. After treatment, they will become dust dry in approx. two days and maybe cleaned gently with a soft brush, damp cleaning cloth or mop.
* Check the state of the treated surfaces annually but repaint it not too often to avoid the formation of a film on the surface.